BAOT®

BAOT BIOLOGICAL TECHNOLOGY CO.,LTD.

| Add: | No.12 building, Yujing Industry Zone, 106 Qihao Road, Torch Development District, |  |  |  |
| --- | --- | --- | --- | --- |
|  | Zhongshan, Guangdong, China. 528400 |  |  |  |
| Tel: | +86-760-87893825 | +86-760-87893826 |  |  |
| Fax: | +86-760-87893827 |  |  |  |
| Skype: | baotcom |  | 0120 | ISO13485 |
| Website: | www.baot.biz |  | Version: COP-27-PB-06 A/01 |  |

ZCG

Z i r c o n i a	C e r a m i c

Instructions for Use

BAOT®

BAOT®

| Content |  | Characteristic Features |  |
| --- | --- | --- | --- |
|  |  | Life-like shades |  |
| Characteristic Features | 02 |  |  |
|  |  | 1 | . Colorful shades, classic 16 & 26 shades ceramics |
| Application Procedures | 03-07 | 2. Distinct layers & natural colors |  |
| Firing Parameters | 08 | Mechanical properties |  |
| Shade Matching | 09-10 | 1 | . Natural strength |
|  |  | 2 | . Excellent bonding force |
| Troubleshooting Guide | 11-12 |  |  |
| Attention | 13-14 | Optimal compatibility |  |
|  |  | 1 | . Compatible with various Zirconia coping brands |
|  |  | 2 | . Compatible with other brands’ bonding agents |
|  |  | Tiny particle |  |
|  |  | 1. High density, excellent bonding force, high color intensity |  |
|  |  | 2 | . Low shrinkage, one step build up |

01  Content	Characteristic Features  02

Application Procedures

Ceramic layer distribution

Glaze

Enamel Layer	Transparent

Incisal/Enamel

|  | Body Layer |  |  | Dentine |  |
| --- | --- | --- | --- | --- | --- |
|  | Bonding Layer |  |  |  | Dentine |
| Abutment | Zirconia Coping |  |  |  |  |
| tooth |  |  |  |  |  |

*Anterior Teeth Crosscutting Structure

(ceramic layer distribution)

Application procedures

| 1. | Coping treatment |
| --- | --- |
| 2. |  |
|  | Bonding layer |
| 3. | Dentine application |
| 4. | Enamel & Transparent application |
| 5. | Contouring & Glaze application |

BAOT®

Coping treatment & Bonding layer

Checking	BAOT®

Check whether coping design is acceptable in terms of

size, length and thickness by putting coping onto plaster model. If unacceptable, grind or redesign it.

BAOT®	Bonding layer build up

Apply a thin layer of Dentine on coping surface as the bonding layer

before heat treatment. Roughen the coping surface to strengthen the

bonding force between coping and dentine.

BAOT®

Heat treatment

Heat treatment referring to Firing Parameters.

03  Application procedures	Coping treatment & Bonding layer	04

Dentine application

Mixing

Use Modeling Liquid or distilled water to mix Dentine powder until it becomes pasty, as shown in the picture 1& 2.

Mix the Dentine into paste evenly and completely, as shown in the Picture 3. Don’t make it too dry or too wet.

BAOT®	BAOT®	BAOT®

Picture 1	Picture 2	Picture 3

Dentine build up

Judge the size and length of Dentine layer based on adjacent space and occlusion.

BAOT® Due to shrinkage effect after firing, normally Dentine layer shall be 10% larger to compensate the firing shrinkage.

Absorb water during Dentine application, in order to make Dentine paste solid on the coping and to avoid chipping or moving which may lead to cracks, bubbles and mixed shades.

Dentine in interproximal area must be solid and linked, to avoid cracks by firing shrinkage.

Make sure Dentine covers all edges to avoid exposed area caused by firing shrinkage.

BAOT®

Enamel & Transparent application

BAOT®

Apply Enamel to the incisal 1/3.

Use slightly wet brush pen to pull Enamel, making ceramic layers bonded tightly.

BAOT®

Transparent build up

Apply Transparent to the incisal 2/3, covering Enamel.

BAOT®

Firing

Firing according to the Firing Parameters.

If the ceramic is too wet before firing, lengthen the firing time.

BAOT®	Add-on

Use brush to vibrate tweezer slightly and absorb water to make ceramic condensed.

Repeat until no water seep out.

Do not condense too heavily. Avoid ceramic layers collapsing or mixing.

BAOT®

Firing

Add-on firing temperature should lower than the first firing.

Refer to Firing Parameters.

05  Dentine application	Enamel & Transparent application  06

Countouring & Glaze application

Contouring

BAOT®

After firing, use non-contaminated stones, discs, or diamond burs to refine the anatomy. Check whether additional ceramics are needed.

If additional are required, firing temperature should be 5℃-10℃ lower than the first firing.

* Add-on too many times is not recommended, or it may lead to undesired results.

| Glaze Mixing | BAOT® |
| --- | --- |

Mix Glaze powder with Glaze & Stain Liquid, making it pasty &thoroughly. If the glaze paste is too dry or too watery, it may lead to insufficient glossiness.

BAOT®	Coating & Shades matching

Coating should be evenly distributed. Don’t coat it heavily.

Match shades with a SHADE GUIDE.

If required, use the tip of the staining brush to spread a thin film of Stain

Liquid until satisfactory shade is obtained.

Firing	BAOT®

After Glaze application, fire the coping under atmosphere pressure according to the Firing Parameters.

- If ring temperature is higher than the Firing Parameters, it may lead to circular formation and unnatural over-glossy surface and opacity.

- If ring temperature is lower than the recommended parameter, it may lead to matt and rough surface.

BAOT®

Firing Parameters

| Condition | Coping | Body | Add-on | Glaze & Stain |
| --- | --- | --- | --- | --- |
|  | Heat treatment |  |  |  |
| Drying temp.(℃) | 550 | 500 | 500 | 500 |
| Drying time(min) | 2 | 3 | 2 | 2 |
| Heating time(min) | 2 | 3 | 2 | 2 |
| Heating rate(℃/min) | 50 | 50 | 50 | 50 |
| Firing temp.(℃) | 930 | 920 | 910 | 900 |
| Holding time(min) | 1 | 1 | 1 | 1 |
| Cooling time(min) | 4 | 4 | 4 | 4 |
| Cooling temp.(℃) | 550 | 550 | 550 | 550 |
| Vacuum start(℃) | 500 | 500 | 500 | - |
| Vaccum end(℃) | 930 | 920 | 910 | - |

Note:

This Firing Parameters chart is only for reference. Optimal results will be obtained during practical operation.

Firing temperature and holding time shall be adjusted according to furnace condition, crown design and bridge length.

07  Contouring & Glaze application	Firing Parameters	08